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	Field Guide
	

	
	Residual Element Analysis for Hydrofluoric Alkylation Units
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	SciAps offers both XRF and LIBS based instruments. The Z-902 Carbon model is a portable handheld instrument utilizing Laser-induced Breakdown Spectroscopy (LIBS). The system combines a high-energy pulsed laser, Opti-Purge™ on-board argon purge, and multi-spectrometer design to achieve high-resolution data across a wide spectral range. These HH LIBS analyzers reliably and accurately verify materials for use in Hydrofluoric Alkylation Units (HF Alky). The Z-902 Carbon series can reliably and accurately measure C, Cr, Ni, Cu, and V as well as the other elements that are required for carbon equivalent calculation.
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	The SciAps X-550 is a highly portable, purpose- built instrument utilizing X-ray Fluorescence. The systems combine a 50 kV X-ray tube, a silicon drift detector, and compact geometry between the Xray tube and detector to provide accurate and reliable analysis. XRF is a great option for measuring Cr, Ni, Cu, V, and Nb as well as P and S in low residual element material. The combination of the two technologies provides an optimal solution for testing per API 751 – Safe Operation of Hydrofluoric Acid Alkylation Units (HF Alky).
	

	
	With the increasing demand for material traceability and compliance, the verification of mat- erial has become an essential component in reliability and safety programs. As material specifications become more stringent, the need to test these materials becomes increasingly critical. Standards for applications like the API RP-751 Safe Operations of HF Alkylation Process provides guidelines with proven industry practices for the safe operation of HF Alky units. RP-751 represents industry accepted engineering practices and outlines hazard management, operating procedures, personnel protection, materials of construction, inspection, and maintenance techniques.
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	Material chemistry in carbon steel plays a big role in components used HF Alky service. Low Residual Elements (RE) or HF compliant materials are components that meet the elemental low RE restrictions defined in RP-751. Components with a carbon content greater than 0.18% (C) in carbon steels and the combination of the residuals elements, Cr, Ni, and Cu exceeding 0.15% and Nb plus V exceeding 0.03% in HF Alkylation processes will likely experience an accelerated corrosion rate leading to a premature component failure and releasing HF Alky into the atmosphere. Accurately measuring these elements in carbon steel is critical for predicting accelerated corrosion of components in HF Alkylation process units.
	

	
	SciAps understands the need to be able to verify critical chemistries in these components and has a solution to meet your verification needs. SciAps utilizes complementing technologies to accurately measure the restricted residual elements. Utilizing the Z-902 Carbon handheld LIBS and the X-550 Handheld XRF, you can confidently and accurately measure the Low RE restrictions in your HF Alky components. Below you will see the Low RE chemistry requirements for carbon steel material used in HF Alky service. Use this sheet as a quick reference guide to know and understand the elemental restrictions and formulas when analyzing HF Alky material in the field.
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	Quick Reference Field Guide for Analyzing HF Alky Material
	

	
	HF Alkylation (API 751) residual elements:
	

	
	Cu + Ni + Cr < 0.15% with C% >0.18%
	

	
	Cu + Ni < 0.15% with C% <0.18%
	

	
	Nb < 0.02%
	

	
	V < 0.02%
	

	
	Nb + V < 0.03%
	

	[Back]
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	This chart summarizes the “Additional Supplementary Requirements”
	

	
	CE
	

	
	< 0.43¹<0.45²
	

	
	C
	

	
	> 0.18%
	

	
	P
	

	
	<0.01%
	

	
	S
	

	
	<0.015%
	

	
	Ni+Cu³
	

	
	< 0.15%
	

	
	Cr+Ni+Cu⁴
	

	
	< 0.15%
	

	
	V
	

	
	< 0.02%
	

	
	Nb
	

	
	< 0.02%
	

	
	V+Nb
	

	
	< 0.03%
	

	
	¹Material thickness is < 1”
	

	
	²Material thickness is > 1”
	

	
	³Material thickness is < 1”
	

	
	⁴When Carbon content is > 0.18
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	The Z-902 Carbon and X-550 have industry leading Limits of Detection (LOD) to be able to accurately measure those low RE elements needed to verify HF compliant components. The LOD are listed below for each technology.
	

	
	Instrument LOD
	

	
	Technique
	

	
	LIBS Z-902 C
	

	
	XRF X-550
	

	
	C
	

	
	0.007%
	

	
	n/a
	

	
	Cr
	

	
	0.015%
	

	
	0.003%
	

	
	Ni
	

	
	0.015%
	

	
	0.02%
	

	
	Cu
	

	
	0.01%
	

	
	0.002%
	

	
	V
	

	
	0.01%
	

	
	0.002%
	

	
	Nb
	

	
	0.02%
	

	
	0.001%
	

	
	P
	

	
	n/a
	

	
	0.01%
	

	
	S
	

	
	n/a
	

	
	0.015%
	

	
	Carbon Equivalent (CE) is also a crucial part of the Supplementary Requirements
	

	
	(see note S54.2 above)
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	CE
	

	
	Weldability
	

	
	Up to 0.35
	

	
	0.36–0.40
	

	
	0.41–0.45
	

	
	0.46–0.50
	

	
	Over 0.50
	

	
	Excellent
	

	
	Very good
	

	
	Good
	

	
	Fair
	

	
	Poor
	

	
	Carbon Equivalency (IIW) most common:
	

	

	CE = C + (Mn/6) + (Cr + Mo + V)/5 + (Cu + Ni)/15
	

	
	Carbon Equivalent (AWS):
	

	
	CE = C + (Mn + Si)/6 + (Cr + Mo + V)/5 + (Cu + Ni)/15
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	Summary
	

	
	With the demanding compliance restrictions for HF Alky material the SciAps Z-902 Carbon LIBS and X-550 can measure Low RE material while simultaneously determining CE in the field, helping you to identify potential rogue material or verify HF compliant material efficiently and accurately. By utilizing these two portable and incredibly fast technologies, you can be assured that you are meeting or exceeding the requirements in your reliability and safety program.
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	YouTube.com/SciAps
	




image4.png
The SciAps X-550 is a highly portable, purpose-
built instrument utilizing X-ray Fluorescence. The
systems combine a 50 kV X-ray tube, a silicon drift
detector, and compact geometry between the X-
ray tube and detector to provide accurate and
reliable analysis. XRF is a great option for
measuring Cr, Ni, Cu, V, and Nb as well as P and S in
low residual element material. The combination of
the two technologies provides an optimal solution
for testing per APl 751 - Safe Operation of
Hydrofluoric Acid Alkylation Units (HF Alky).

LIBS

TECHNOLOGY

With the increasing demand for material
traceability and compliance, the verification of mat-
erial has become an essential component in reliability and safety programs. As material
specifications become more stringent, the need to test these materials becomes increasingly
critical. Standards for applications like the APl RP-751 Safe Operations of HF Alkylation Process
provides guidelines with proven industry practices for the safe operation of HF Alky units. RP-751
represents industry accepted engineering practices and outlines hazard management, operating
procedures, personnel protection, materials of construction, inspection, and maintenance techniques.
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Material chemistry in carbon steel plays a big role in components used HF Alky service. Low Residual Elements (RE) or HF
compliant materials are components that meet the elemental low RE restrictions defined in RP-751. Components with a carbon
content greater than 0.18% (C) in carbon steels and the combination of the residuals elements, Cr, Ni, and Cu exceeding 0.15%
and Nb plus V exceeding 0.03% in HF Alkylation processes will likely experience an accelerated corrosion rate leading to a
premature component failure and releasing HF Alky into the atmosphere. Accurately measuring these elements in carbon steel is
critical for predicting accelerated corrosion of components in HF Alkylation process units.

SciAps understands the need to be able to verify critical chemistries in these components and has a solution to meet your
verification needs. SciAps utilizes complementing technologies to accurately measure the restricted residual elements. Utilizing
the Z-902 Carbon handheld LIBS and the X-550 Handheld XRF, you can confidently and accurately measure the Low RE
restrictions in your HF Alky components. Below you will see the Low RE chemistry requirements for carbon steel material used
in HF Alky service. Use this sheet as a quick reference guide to know and understand the elemental restrictions and formulas
when analyzing HF Alky material in the field.
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Quick Reference Field Guide for Analyzing HF Alky Material

HF Alkylation (API 751) residual elements: ADDITIONAL SUPPLEMENTARY REQUIREMENTS
Cu + Ni + Cr < 0.15% with C% >0.18%
Cu + Ni < 0.15% with C% <0.18%
Nb < 0.02%
V< 0.02%
Nb +V < 0.03%

In addition, the following supplementary requirement is suitable for this application.

§54. Requirements for Carbon Steel Plate for Maximum niobium = 0.02%
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This chart summarizes the “Additional Supplementary Requirements”
CE C P S Ni+Cu® Cr+Ni+Cu* \% Nb V+Nb
< 0.43'<0.452 > 0.18% <0.01% <0.015% < 0.15% < 0.15% < 0.02% < 0.02% < 0.03%

"Material thickness is < 17
2Material thickness is > 17
*Material thickness is < 17
“When Carbon content is > 0.18
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The Z-902 Carbon and X-550 have industry leading Limits of Detection (LOD) to be able to accurately measure those low RE
elements needed to verify HF compliant components. The LOD are listed below for each technology.

Instrument LOD

Technique C Cr Ni Cu \% Nb P S
LIBS Z-902 C 0.007% 0.015% 0.015% 0.01% 0.01% 0.02% n/a n/a
XRF X-550 n/a 0.003% 0.02% 0.002% 0.002% 0.001% 0.01% 0.015%

Carbon Equivalent (CE) is also a crucial part of the Supplementary Requirements
(see note S54.2 above)
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Carbon Equivalency (IIW) most common:
CE =C+ (Mn/6) + (Cr + Mo + V)/5 + (Cu + Ni)/15

Carbon Equivalent (AWS):
CE=C+ (Mn+Si)/6 + (Cr + Mo + V)/5 + (Cu + Ni)/15

CE Weldability
Up to 0.35 Excellent
0.36-0.40 Very good
0.41-0.45 Good
0.46-0.50 Fair
Over 0.50 Poor
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Summary

With the demanding compliance restrictions for HF Alky material the SciAps Z-902 Carbon
LIBS and X-550 can measure Low RE material while simultaneously determining CE in the
field, helping you to identify potential rogue material or verify HF compliant material
efficiently and accurately. By utilizing these two portable and incredibly fast technologies,
you can be assured that you are meeting or exceeding the requirements in your reliability
and safety program.
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SciAps offers both XRF and LIBS based instruments. The Z-902 Carbon model is a
portable handheld instrument utilizing Laser-induced Breakdown Spectroscopy
(LIBS). The system combines a high-energy pulsed laser, Opti-Purge™ on-board
argon purge, and multi-spectrometer design to achieve high-resolution data across
a wide spectral range. These HH LIBS analyzers reliably and accurately verify
materials for use in Hydrofluoric Alkylation Units (HF Alky). The Z-902 Carbon
series can reliably and accurately measure C, Cr, Ni, Cu, and V as well as the other
elements that are required for carbon equivalent calculation.




