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	Advantages of 55kV pXRF Over Conventional 50kV pXRF
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	Pushing the limits of field geochemical analysis
	

	
	Once again the team at SciAps forges ahead into new territory with their new X-555 55kV pXRF. Initially imagined to further compliment SciAps continued commitment to building new tools to aid in the analysis of critical metals and the green economy transition, they have been busy investigating how this makes a difference in a variety of settings.
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	The 55kV difference
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	Fig. 1. Estimated LOD’s based on analytical performance of both X-505 and X-555 testing a mix of Certified Reference Materials (CRMs) representing a wide range of matrix types.
	

	
	The range of mineralization styles being targeted for critical minerals creates various analytical challenges. SciAps unique 55kV pXRF, with lower detection limits on a range of important elements, significantly improves the suitability of pXRF for numerous applications. The 55kV excitation allows for the effective differentiation of many key elements from background concentrations than with conventional pXRF.
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	Rare Earth Elements (REE)
	

	
	A significant proportion of global REE supply comes from Ion Adsorption Clays (IAC) and Alkaline Igneous rocks that can contain economic, but generally lower, REE concentrations to other common sources of REE such as weathered carbonatites and placer deposits. The lower concentration ranges being encountered present challenges using 50kV approaches to REE analysis. Please see examples below of data generated using SciAps X-505 vs X-555 on some of the common light REE analyzed by both 50kV and 55kV pXRF.
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	Fig. 2. LREE Ce performance improvements are obvious both in relation to lower detection limits and improved accuracy.
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	Pathfinder elements for base and precious metals
	

	
	Exploration for precious and base metals often relies on pathfinder elements to identify styles of mineralization and define zonation around ore forming systems. Improved performance for Ag, Te, Sn, Sb, Ba, Cd further enhances the ability of pXRF to better define anomalies through better definition of those elements at low concentrations in addition to the other important pathfinder elements already analysed at 40kV and other lower energy beam settings.
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	Fig. 3. Ag performance improvements are obvious both in relation to lower detection limits and improved accuracy. In addition to being a valuable primary target element, it is also important in Au and base metal systems as well.
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	LCT pegmatites
	

	
	The improved performance on Cs and Sn as well as other important elements in the LCT suite (Li Cs Ta) and pathfinder elements such as Ta, Nb and Rb.
	

	
	This is also complimented further by SciAps unique handheld Z-900 series LIBS for Li (Z-901 and Z-903) and other important elements such as Be and B (Z903 only). SciAps is the only company offering best in class pXRF and LIBS with capabilities to merge pXRF and LIBS datasets to complete your geochemical suite.
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	Fig. 4. Tellurium (Te) performance demonstrated on OREAS 600 series CRMs. 50kV performance for Te is generally inadequate to allow definition of anomalies due to it being often present at low concentrations.
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Pushing the limits of field geochemical analysis
Once again the team at SciAps forges ahead into new territory with their new X-555 55kV pXRF. Initially imagined to

further compliment SciAps continued commitment to building new tools to aid in the analysis of critical metals and the
green economy transition, they have been busy investigating how this makes a difference in a variety of settings.
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The 55kV difference
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Fig. 1. Estimated LOD’s based on analytical performance of both X-505
and X-555 testing a mix of Certified Reference Materials (CRMs)
representing a wide range of matrix types.

The range of mineralization styles being targeted for critical
minerals creates various analytical challenges. SciAps’
unique 55kV pXRF, with lower detection limits on a range of
important elements, significantly improves the suitability of
pXRF for numerous applications. The 55kV excitation allows
for the effective differentiation of many key elements from
background concentrations than with conventional pXRF.
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Rare Earth Elements (REE)

A significant proportion of global REE supply comes from
lon Adsorption Clays (IAC) and Alkaline Igneous rocks that
can contain economic, but generally lower, REE
concentrations to other common sources of REE such as
weathered carbonatites and placer deposits. The lower
concentration ranges being encountered present challenges
using 50kV approaches to REE analysis. Please see
examples below of data generated using SciAps X-505 vs
X-555 on some of the common light REE analyzed by both
50kV and 55kV pXRF.
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Fig. 2. LREE Ce performance improvements are obvious both in
relation to lower detection limits and improved accuracy.
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Pathfinder elements for base and precious metals

Exploration for precious and base metals often relies on pathfinder elements to identify styles of mineralization and
define zonation around ore forming systems. Improved performance for Ag, Te, Sn, Sb, Ba, Cd further enhances the
ability of pXRF to better define anomlies through better definition of those elements at low concentrations in addition
to the other important pathfinder elements already analysed at 40kV and other lower energy beam settings.
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Fig. 3. Ag performance improvements are obvious both in
relation to lower detection limits and improved accuracy. In
addition to being a valuable primary target element, it is also
important in Au and base metal systems as well.
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LCT pegmatites

The improved performance on Cs and Sn as well as
other important elements in the LCT suite (Li Cs Ta)
and pathfinder elements such as Ta, Nb and Rb.

This is also complimented further by SciAps unique
hand held Z-900 series LIBS for Li (Z-901 and Z-903)
and other important elements such as Be and B (Z-
903 only). SciAps is the only company offering best
in class pXRF and LIBS with capabilities to merge
pXRF and LIBS datasets to complete your
geochemical suite.
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Fig. 4. Tellurium (Te) performance demonstrated on OREAS 600 series
CRMs . 50kV performance for Te is generally inadequate to allow definition
of anomalies due to it being often present at low concentrations.
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